# In-Situ Concrete Strength Verification and Crane-Above-Formwork SIMOPS Controls

## Executive position

Do not approve shoring or strut removal solely from a rebound-hammer or ultrasonic-pulse-velocity reading. The required stage strength and the full permanent load path must be defined by the structural engineer and temporary-works designer. The release decision must then be supported by accepted concrete evidence, current monitoring and groundwater status, the approved removal sequence, and a formal written staged release.

The official Abu Dhabi falsework code requires the concrete to have reached its required design strength, with strength checked to engineering requirements—normally by testing-laboratory cube tests—before a permit to strike is issued. 1 Dubai requires written consultant consent before anchor removal. 2 The public sources reviewed do not prescribe one universal Dubai Municipality or Abu Dhabi DMT NDT method for every shoring-release stage. Therefore, the appointed structural engineer, temporary-works designer, consultant, issued building permit and any development-zone condition determine whether NDT, cores or both are required for the particular release.

## 1. Third-party laboratory accreditation: what to require

| Requirement | Dubai / Abu Dhabi application | Evidence to obtain before testing | Release implication |
| --- | --- | --- | --- |
| ISO/IEC 17025:2017 accredited testing laboratory | Dubai Central Laboratory is accredited by EIAC to ISO/IEC 17025 for testing/calibration, including Infrastructure and Building Materials Laboratories. 3 ENAS is the UAE national accreditation system for ISO/IEC 17025 testing laboratories. 4 Abu Dhabi’s Central Testing Laboratory provides services to ISO 17025:2017 and uses accredited private-sector laboratory partners for building-materials and construction testing. 5 | Current accreditation certificate, expiry date, accreditation-body identification and the laboratory’s current scope. | Treat an unaccredited or out-of-scope report as insufficient unless the consultant/authority gives written project-specific acceptance. |
| Accredited scope covers the exact method | The lab must be accredited for the relevant concrete method—not merely hold generic ISO/IEC 17025 accreditation. | Scope schedule identifying the method, material/matrix and test range, such as core strength, rebound number, UPV or maturity. | If the required method is outside the laboratory’s scope, obtain an authority/consultant-approved alternate laboratory or specific acceptance before relying on the result. |
| Competent testing personnel and calibrated equipment | ISO/IEC 17025 competence requires personnel, equipment control, traceability, internal quality control and valid reporting. 4 | Technician competence/authorisation record, equipment identification, in-date calibration/verification certificates, pre-use checks and any NDT reference anvil/check results. | The test result must be traceable to a competent operator and controlled equipment. |
| Municipality / permit / consultant acceptance | A municipal or development-zone permit can impose more stringent requirements than the general accreditation framework. DMT/DM public material does not create a single identical construction-stage submission route for all projects. | Issued permit conditions, consultant-approved ITP, approved test plan, third-party appointment (if required), and written acceptance route. | The project team must not assume that EIAC/ENAS accreditation alone satisfies a named authority or consultant condition. |

Practical procurement clause: “Appoint a third-party laboratory accredited to ISO/IEC 17025:2017 by ENAS, EIAC or another accreditation body accepted in writing by the relevant authority/consultant, with a current accredited scope expressly covering each proposed test method. Submit the certificate and scope before mobilisation.”

## 2. Test-method hierarchy for a shoring-release decision

| Evidence tier | Applicable method / standard | Appropriate use | Limitation / release condition |
| --- | --- | --- | --- |
| Primary production evidence | Traceable cured cubes in accordance with the project specification and laboratory method; Abu Dhabi CoP 40.0 identifies laboratory cube testing as the normal route. 1 | Verifies the actual mix/pour against the designer’s specified stage-strength criterion. | The sample must be traceable to the actual pour and test age. A cube result does not, by itself, confirm the full wall/slab load path, water condition or support-system readiness. |
| Early-age strength support | Concrete maturity method, ASTM C1074, only where an approved strength–maturity relationship for the project mixture is established. | Can support earlier decision-making where the project-specific calibration and field temperature history are valid. | It does not replace the approved acceptance method unless the structural engineer/consultant explicitly authorises it for the stage. |
| Indirect NDT – rebound hammer | ASTM C805/C805M or EN 12504-2. | Surface uniformity screening, comparative mapping and selection of locations for additional investigation. | Rebound number is not a stand-alone compressive-strength acceptance value; surface condition, carbonation, moisture, aggregate and orientation affect results. Use an engineer-approved correlation. |
| Indirect NDT – ultrasonic pulse velocity (UPV) | ASTM C597 or EN 12504-4. | Evaluates relative uniformity, potential discontinuities and changes in concrete quality; useful alongside rebound mapping. | UPV is not a direct compressive-strength test. Do not convert a velocity directly into release strength without a valid project-specific correlation and engineer acceptance. |
| Complementary indirect method | Penetration resistance, ASTM C803/C803M, or pull-out testing, ASTM C900, where selected by the engineer. | May provide additional early-age/in-place information in a project-specific test plan. | The method, sampling density and acceptance interpretation must be selected by the structural engineer; repair of test locations must be included in the procedure. |
| Direct in-place strength evidence | Extracted cores, ASTM C42/C42M or EN 12504-1; assessment to the project’s applicable structural-code/specification requirements. | Resolves doubt where cubes are unrepresentative, results are low/inconsistent, or NDT suggests variability. | Core location, size, reinforcement scanning, repair and structural implications must be approved before drilling. Core results require engineering interpretation; do not apply generic acceptance values without the project code/specification. |
| Interpretation framework | ACI 228.1R is a recognised engineering reference for in-place concrete-strength estimation; it supports a combined, correlation-led approach. | Guides the engineer in combining NDT and direct evidence. | It is not, by itself, a municipality permit or a release authorisation. The project design and consultant approval remain controlling. |

## 3. Minimum NDT / in-situ verification plan

| Plan component | Required detail |
| --- | --- |
| Engineering question | State whether the purpose is early-age strength, uniformity mapping, investigation of a questionable cube result, confirmation of a completed load path, or a specific shoring-release criterion. |
| Approved acceptance criterion | The structural engineer and temporary-works designer must state the stage-specific target and acceptance logic before testing. Do not choose the criterion after seeing results. |
| Test grid and locations | Mark locations on the structural drawing. Avoid edges, honeycombing, construction-joint anomalies, obvious repair areas and reinforcement where the selected method requires it. Use reinforcement scanning before coring. |
| Correlation and environmental controls | Record mix, age, curing, moisture, surface preparation, member geometry, test orientation and temperature. For indirect NDT, provide the project-specific correlation basis and its applicability. |
| Sampling density | Set the number and distribution of readings/cores in the approved test plan. Increase coverage where results are variable, the support-release consequence is high, or the wall/slab is structurally non-uniform. |
| Data traceability | Record technician, method, instrument serial number, calibration/verification status, date/time, raw readings, photo, grid reference and any deviation. |
| Engineer’s conclusion | The final report must state the limitations and whether the combined evidence satisfies the named stage criterion. The laboratory reports data; the structural/temporary-works design authorities approve the load-transfer release. |

## 4. Reports and sign-offs before release

| Required document | Must contain | Sign-off / acceptance |
| --- | --- | --- |
| Laboratory prequalification pack | ISO/IEC 17025 certificate, scope, competent personnel, method capability and equipment calibration/verification. | Consultant / project QA-QC; authority only if permit condition requires. |
| Approved test method statement | Purpose, member/stage, test standards, locations, correlation, core repair, HSE controls and data-quality controls. | Structural engineer; temporary-works designer where release is linked to support removal; consultant. |
| NDT field report | Method, standard, reading grid, raw readings, instrument ID, calibration/verification, photos, environmental/surface condition and limitation statement. | Laboratory authorised signatory; structural engineer review. |
| Core report, if required | Core ID/location, diameter/length, conditioning, test method, measured strength, test date and repair record. | Laboratory authorised signatory; structural engineer interpretation. |
| Combined strength assessment | Reconciles cubes, maturity (if used), NDT and cores; compares the evidence with the specified stage criterion; identifies uncertainty and conclusion. | Structural engineer; consultant. |
| Temporary-works staged release | Identifies exact strut/anchor/shoring member(s), removal order, retained supports, monitoring actions, water-control assumptions, exclusion zone and stop-work triggers. | Temporary-works designer/coordinator; consultant; written consent for Dubai anchor removal. 2 |
| PTW/SIMOPS revalidation | Current excavation permit, support-change permit/authorisation, lifting plan, exclusion plan, workforce briefing and emergency controls. | Authorised permit issuer and Principal Contractor. |

## 5. Daily SIMOPS coordination checklist: heavy cranes above active internal formwork floors

Default rule: Do not allow formwork, reinforcement, concreting or other work beneath a suspended load, within the crane’s lift/fall zone, or inside a floor area affected by unverified crane/landing/platform loads. If a lift must traverse the floor, clear and barricade the affected zone, freeze the conflicting work and release the area only after the lifting supervisor gives an all-clear.

### A. Shift-start governance

| Check | Yes / No / N.A. | Evidence / action if No | Owner |
| --- | --- | --- | --- |
| A1. One named SIMOPS coordinator has been appointed for the shift with authority to stop each conflicting activity. |  |  | Principal Contractor |
| A2. Daily activity map identifies crane position, radius, lift corridor, landing zone, plant routes, formwork/rebar workfaces, duty/standby pumps and evacuation routes. |  |  | SIMOPS Coordinator |
| A3. All active permits, lift plans, formwork permits, PTWs and inspection releases are current for the named workface. |  |  | Permit Issuer / HSE |
| A4. Shift handover has identified retained/removed supports, incomplete lifts, current monitoring/water status and outstanding hold points. |  |  | Shift Supervisors |
| A5. A single radio channel and standard communications protocol have been tested between lifting, formwork, earthworks, dewatering and emergency leads. |  |  | Lifting Supervisor |

### B. Crane, ground and lift-plan controls

| Check | Yes / No / N.A. | Evidence / action if No | Owner |
| --- | --- | --- | --- |
| B1. Crane certification, operator/rigger/slinger competence and lifting-accessory inspection are valid. |  |  | Appointed Person |
| B2. The lift plan matches the actual load, radius, boom configuration, wind condition, travel route and landing location. |  |  | Appointed Person |
| B3. The crane, outrigger, track or support position has an accepted bearing and surcharge check against the temporary-works design. |  |  | Temporary-Works / Geotechnical Authority |
| B4. The planned lift path does not pass over occupied formwork, rebar, concrete-pour or access/egress areas. |  |  | Lifting Supervisor |
| B5. The lift is classified as routine, non-routine or critical under the project procedure; the required additional authorisation is attached. |  |  | Appointed Person |
| B6. Wind, visibility, lighting and weather conditions comply with the lift plan/manufacturer limits and site procedure. |  |  | Crane Operator / Lifting Supervisor |
| B7. Blind-lift controls, banksman location, signal method and communication test are confirmed. |  |  | Lifting Supervisor |

### C. Formwork, floor and structural-work controls

| Check | Yes / No / N.A. | Evidence / action if No | Owner |
| --- | --- | --- | --- |
| C1. The formwork/falsework is in the approved configuration and its permit to load / pre-pour release remains valid. |  |  | Formwork Supervisor / Consultant |
| C2. The floor/work platform capacity has been checked for the planned landing, stored material, crane-induced load, dynamic effect and route. |  |  | Structural / Temporary-Works Designer |
| C3. No falsework, scaffold, deck or temporary platform will be struck, altered, overloaded or used as a lifting landing area without the approved design and release. |  |  | Formwork Supervisor |
| C4. Rebar and formwork crews understand the work freeze, exclusion boundary and all-clear handback method. |  |  | Structural Work Supervisor |
| C5. A protected evacuation route remains open; neither lifting gear, delivered materials nor temporary services obstruct it. |  |  | SIMOPS Coordinator |

### D. Workface segregation and active lifting controls

| Check | Yes / No / N.A. | Evidence / action if No | Owner |
| --- | --- | --- | --- |
| D1. Physical barriers, signs and a sentry/spotter isolate the lift/fall zone from the active formwork floor. |  |  | Lifting Supervisor |
| D2. The affected floor is cleared before the load enters the lift/fall zone; no person is beneath the suspended load. |  |  | Formwork + Lifting Supervisors |
| D3. Earthmoving, telehandler, concrete pump or delivery activity is frozen where it can interfere with crane stability, lift route or evacuation. |  |  | SIMOPS Coordinator |
| D4. Tag lines, load-control method and landing-zone controls are in place; hands are clear of crush/pinch points. |  |  | Rigger / Slinger |
| D5. No lift begins until the lifting supervisor confirms “zone clear”; no structural work resumes until a documented “all clear” is given. |  |  | Lifting Supervisor |

### E. Water, monitoring and emergency readiness

| Check | Yes / No / N.A. | Evidence / action if No | Owner |
| --- | --- | --- | --- |
| E1. Duty and standby dewatering pumps are operational; no isolation/work on a pump jeopardises excavation stability. |  |  | Dewatering Supervisor |
| E2. Latest instrumentation and visual inspection status show no unresolved movement, groundwater or support-system trigger. |  |  | Monitoring / Temporary-Works Authority |
| E3. Emergency access, rescue equipment, first aid, alarm method and site emergency contacts are available and unobstructed. |  |  | HSE Lead |
| E4. A stop-work and revalidation protocol is understood for high wind, rain/flooding, pump fault, monitoring alert, support damage, crane fault or lost communications. |  |  | SIMOPS Coordinator |

## 6. Crane/formwork permit-interface matrix

| Work interface | Controlling document | Linked permit / release | Required acceptance before work | Stop / revalidate trigger |
| --- | --- | --- | --- | --- |
| Crane lift above/adjacent to internal formwork floor | Approved lift plan under CoP 34.0. 6 | Routine/critical-lift authorisation as defined by project procedure; daily SIMOPS release. | Load, radius, route, crane position, ground bearing, exclusion zone and floor clearance accepted. | Lift path, load, radius, crane position, wind, communications or occupancy changes. |
| Active formwork/falsework below crane influence area | Formwork/falsework design and CoP 40.0 permit-to-load/permit-to-strike process. 1 | Pre-pour/permit-to-load release; controlled workface handback. | Floor/falsework capacity, configuration, inspection status, protected egress and worker briefing accepted. | Formwork alteration, overloading, incomplete inspection, damaged deck or lift-zone intrusion. |
| Excavation and temporary shoring | Excavation PTW and approved temporary-works/dewatering/monitoring plan. | Stage-release permit for any support change; monitoring review. | Shoring condition, surcharge/bearing, groundwater and monitoring trends acceptable. | Trigger breach, water event, plant relocation, support defect or unapproved load. |
| Crane setup / outriggers near excavation | Lift plan + temporary-works bearing/surcharge check. | Plant-position release / ground-bearing certificate as project procedure requires. | Designer-accepted set-back, mat/base-plate design, actual ground condition and exclusion area. | Ground deterioration, settlement, rain, position change or monitoring concern. |
| Electrical / dewatering system conflict | Electrical PTW and CoP 24.0 LOTO isolation certificate, linked to dewatering-resilience plan. | Isolation certificate / LOTO; standby pumping verification. | Alternative pumping/backup and water-level controls verified before isolation. | Loss of backup, water-level rise, electrical fault or maintenance delay. |
| Hot work / welding near formwork or waterproofing | Hot-work PTW and fire-prevention controls. | Hot-work permit; fire-watch release. | Combustibles controlled, ventilation/atmosphere acceptable and escape route open. | Change in atmosphere, fire-watch absence, water/flooding or fire-protection impairment. |
| Work at height / leading-edge work | Working-at-height plan and scaffold/formwork inspection status. | Work-at-height permit where required by project system; rescue plan. | Certified access, edge protection, anchor/rescue system and no lift conflict. | Incomplete guardrail, scaffold/formwork change, wind condition or lift-zone encroachment. |
| Concrete placement after lifting | Concrete-pour plan, CoP 38.0 and formwork permit-to-load. 7 | Pre-pour ITP release; concrete-pump setup approval. | Formwork capacity, pump position, truck route, hose restraint, evacuation route and dewatering readiness accepted. | Pump or truck relocation, hose conflict, formwork distress, weather/water event or loss of egress. |

## 7. Non-negotiable work rules

| Rule | Project-manager instruction |
| --- | --- |
| No work beneath a suspended load | Clear and barricade the floor area before the lift; do not substitute administrative warnings for physical segregation. |
| No crane/plant position by convenience | Obtain the temporary-works/geotechnical acceptance for bearing, surcharge, set-back and route. |
| No NDT-only release | Use NDT as the approved test plan permits; require engineering interpretation and direct evidence where the result is uncertain or high consequence. |
| No support change by verbal agreement | Require the written staged release, linked PTW revalidation and consultant consent where required. |
| No SIMOPS without a single coordinator | The Principal Contractor appoints one coordinator to control schedules, zones, interfaces, handover and stop-work authority. |

## References